THIS SHEET IS ONLY A PLACE HOLDER.

PLEASE REPLACE IT WITH

THE SWRMC COVER SHEET.

INSTRUCTIONS:

There could be minor differences that each Company may use to accomplish the same goal of the PCP.   Therefore, our ultimate goal is to develop a PCP which is generic enough for all Companies to use.

Forms/PCP may be modified to the welding attribute required.

Forms shall be marked Not Applicable when not in use

PCP REVISION: RECORD OF CHANGES

| Ship Hull: |  |  |  | PCP #: |  | Contract#: |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Job#: |  |  |  | Work Item/Mod: |  |  |  |  |
| Rev |  | Description |  |  |  |  | Pen Ink Y/N | Date |
| Personally Verified Pen and Ink Changes |  |  |  |  |  |  |  |  |
| REV | SWRMC Code |  | Name Print |  | Signature |  |  | Date |

PROCESS CONTROL PROCEDURE FOR

WELDING CLASS P-1 PIPING

TABLE OF CONTENTS

| # SECTION |  | PAGE |
| --- | --- | --- |
|  | PCP REVISION: RECORD OF CHANGES……………………………….. | 2 |
|  | TABLE OF CONTENTS / APPENDICE / ENCLOSURES……………….. | 3-4 |
|  | SCOPE.………………………………………………………………….......... | 5-6 |
|  | PURPOSE…………………………………………………………………….. | 6 |
|  | REFERENCES | 6 |
|  | QUALIFICATION REQUIREMENTS………………………………………. | 6 |
|  | DIRECT KNOWLEDGE….…………………………………………..………. | 7 |
|  | MATERIAL/EQUIPMENT………………………………….………..……….. | 7 |
|  | SAFETY EQUIPMENT……………..………………………………..………. | 7 |
|  | SAFETY PRECAUTIONS…………..……………………………………...... | 8 |
|  | PREPARATION…….…..………………...…………………….…………….. | 9 |
|  | START OF PROCEDURE…………………………………………………. | 9 |
|  | FITUP REQUIREMENTS..……………………………..………................... | 9-10 |
|  | CLEANING REQUIREMENTS…..………………………………...……….. | 10 |
|  | WELDING TECHNIQUE………………...…………………………..……… | 10 |
|  | WELDING INSPECTION REQUIREMENTS……………………............... | 10-11 |
|  | PREHEAT AND INTERPASS TEMPERATURE…………………………. | 11 |
|  | PRESSURE TESTING……....………………….………………...…………. | 11 |
|  | INSPECTION/DOCUMENTATION FORMS……….……….……………... | 11 |
|  | OBJECTIVE QUALITY EVIDENCE………………………………………... | 12 |
|  | CONTROL OF THE PROCEDURE…………………………………........... | 12 |
|  | HAZARDOUS MATERIAL…………………………………………………… | 12 |

| # appendices |  | PAGE |
| --- | --- | --- |
|  | PCP Direct Knowledge Attendance Form………………………………….. | A-1-1 |
|  | Weld Technique Sheet …..….……………………...……………….………. | A-2-1 |
|  | Weld Inspection and Testing Requirements………………………………. | A-3-1 |
|  | Pipe Fit-up Inspection Record………………………………………………. | A-4-1 to A-4-3 |
|  | Joint Design……………………………………………………………........... | A-5-1 |
|  | Joint Map……………………………………………………………………… | A-6-1 |
|  | Preheat/Interpass Temperature Record…………………………………… | A-7-1 |
|  | Weld In-Process Control/NDT Record……………………………………… | A-8-1/2 |
|  | Weld Defect Repair Record…………………………………………………. | A-9-1 |
|  | Welded Joint Backing Ring Dimension……………………………………. | A-10-1 |

| ENCLOSURES |  | PAGE |
| --- | --- | --- |
|  | Work Item / RCC’s / IDR’s. ..………………………………………………… | E-1-1 to |
|  | Welder Qualifications……………….……………………………………….. | E-2-1 to |
|  | NDT Inspector Qualifications……………………………………………….. | E-3-1 to |
|  | Hydrostatic Test Record / Operational Pressure Test Record…….…….. (as applicable) | E-4-1 to |
|  | Pipe Bend Records (When Applicable will be self-provided).…………… | E-5-1 to |

# SECTION 1 IDENTIFICATION

## SCOPE

### This procedure is applicable for welding on Class P-1 Piping Systems (except for titanium and its alloys). This procedure meets the requirements of References (a) through (h) and (Enclosure 1), located in (Ship’s Space) aboard (Ships name and hull number).

NOTE 1: PROCESS CONTROL PROCEDURES (PCPS) ARE SWRMC CODE 200 APPROVED DOCUMENTS FOR CONTRACTOR EXECUTION OF A SPECIFIC REPAIR ITEM. PCPS ARE TO BE FOLLOWED AS WRITTEN. HOWEVER THERE MAY BE CIRCUMSTANCES WHERE THE PCP NEEDS TO BE REVISED TO MEET FIELD CONDITIONS. REVISIONS THAT IN THE OPINION OF THE SWRMC ONSITE REP AND THE SWRMC CODE 200 SIGNATORY ARE MINOR AND DO NOT DEGRADE THE OVERALL PERFORMANCE OF THE PROCESS, REQUIRE CONTRACT MODIFICATIONS, OR SIGNIFICANTLY ALTER THE SCOPE OF THE WORK MAY BE MADE ONSITE BY THE SWRMC ONSITE REP WITH CONCURRENCE OF THE SWRMC CODE 200 PCP SIGNATORY. CHANGES WILL BE NOTED WITH NAME, TIME, DATE AND SIGNATURE OF SWRMC CODE 200/ONSITE REP MAKING THE CHANGE ON THE KTR'S COPY OF THE PCP AS PEN-AND-INK CHANGES. THE KTR WILL SUBMIT A FORMAL REVISION WITHIN 3 WORKING DAYS OF THE PEN-AND-INK CHANGE. THE PCP REVISION POLICY IS STATED IN SWRMC SOP-225-002(SEE NOTE 2 BELOW FOR REVISION INSTRUCTIONS)

NOTE 2: PCP REVISIONS SHALL BE SUBMITTED UNDER A NEW COVERSHEET AND INCLUDE ONLY THOSE PCP PAGES CHANGED OR ADDED BY THE REVISION ON THE REVISION SHEET (RECORD OF PAGE CHANGES).  EACH PCP REVISION SHALL ALSO PROVIDE A NEW DIRECT KNOWLEDGE ATTENDANCE FORM (APPENDIX 1).

RECORD OF PAGE CHANGES: THIS SHEET WILL BE PLACED AFTER THE REVISED PCP COVERSHEET AND SHALL DOCUMENT EACH NEW OR CHANGED PAGE FROM THE APPROVED PCP. THE SHEET WILL LIST EACH AFFECTED PAGE, A SUMMARY OF THE CHANGES, AND REASON FOR THE CHANGE. SUBSEQUENT REVISIONS WILL BE RECORDED ON THE SAME RECORD OF PAGE CHANGES SHEET USING THE NEXT REVISION LETTER/NUMBER AND SUBMITTED UNDER A NEW COVERSHEET. THIS PRACTICE WILL REDUCE THE SIZE OF PCP REVISION DOCUMENTATION WHILE ENSURING PCP OBJECTIVE QUALITY EVIDENCE (OQE) REMAINS INTACT ACROSS PCP REVISIONS.

CHANGE PAGES: A PCP REVISION SUBMITTAL NEED PROVIDE ONLY THOSE PAGES CHANGED OR ADDED BY THE REVISION. THE REVISION LETTER SHALL BE ENTERED ON ALL CHANGED PAGES OF THE PCP. NEW PAGES SHALL BE LABELED WITH THE NUMBER OF THE PRECEDING PAGE AND CONSECUTIVELY STARTING WITH "A" (E.G., PAGE 5A OF 15).

PEN AND INK CHANGES SHALL BE ACCOMPLISHED BY DRAWING A SINGLE LINE THROUGH THE PORTION TO BE CHANGED, AND ENTERING THE NECESSARY CHANGE ADJACENT TO THAT PORTION. THE PERSON MAKING THE CHANGE WILL INITIAL, DATE, AND LIST THE REVISION NUMBER. PEN AND INK CHANGES WILL BE PERMANENT ON THE ORIGINAL OQE. THE CHANGE/CORRECTION AND THE PEN AND INK CHANGE(S) SHALL BE VERIFIED BY THE DESIGNATED SWRMC REPRESENTATIVE (SBS, LE, AND CODE 200/135). THIS VERIFICATION WILL BE RECORDED ON THE RECORD OF PAGE CHANGES SHEET.

PEN AND INK CHANGES FOR ENCLOSURE 2 AND ENCLOSURE 3 DO NOT REQUIRE A FORMAL PCP REVISION.

NOTE 3: ANY NONCONFORMING CONDITIONS FOUND DURING THE EXECUTION OF THIS EPCP/PCP (WHICHEVER APPLIES) WILL REQUIRE IMMEDIATE DOCUMENTATION BY THOSE INVOLVED IN PERFORMING OR OVERSEEING THE WORK. THE NONCONFORMING CONDITION MUST BE IMMEDIATELY SUBMITTED TO THE LOCAL TECHNICAL AUTHORITY (SWRMC CHIEF ENGINEER) OR THEIR SIGNATORIES (SWRMC DEPUTY CHIEF ENGINEERS) FOR REVIEW AND FURTHER DIRECTION BEFORE CONTINUATION OF WORK AFFECTED BY THE NONCONFORMING CONDITION."

## PURPOSE

### The purpose of this procedure is to provide a step-by-step process (description) for the welding and fabrication of a P-1 Piping System in accordance with the specifications of (Enclosure 1) and the requirements of References (a) through (f), and Reference (g) and (h) when applicable.

## REFERENCES

### NAVSEA Standard Items

### S9074-AR-GIB-010/278 Requirements for Fabrication welding and Inspection, and Casting Inspection and Repair for Machinery, Piping, and Pressure Vessels

### MIL-STD-22D Welded Joint Design

### T9074-AS-GIB-010/271 Requirements for Nondestructive (NDT) Testing Methods

### MIL-STD-2035A (SH) Nondestructive Testing Acceptance Criteria

### S9074-AQ-GIB-010/248 Requirements for Welding and Brazing Procedure and Performance Qualification

### MIL-STD-1627C Bending of Pipe or Tube for Ship Piping Systems

### S9AAO-AB-GOS-010, General Specifications for Overhaul of Surface Ships (GSO), Section 074

# section 2 PERSONNEL QUALIFICATION

## QUALIFICATION REQUIREMENTS

### Welders will be currently qualified in accordance with Reference (f).  Welder qualifications shall be identified in Enclosure (2). Additions to Enclosure (2) shall be made by “Pen and Ink” and shall be initialed by the Welding Supervisor.

### NDT Inspectors will be qualified in accordance with Reference (d).  NDT Inspector qualifications shall be identified in Enclosure (3). Additions to Enclosure 3 shall be made by “Pen and Ink” and shall be initialed by the appropriate NDT Level III Examiner or his designated representative (i.e. Inspec Testing will change Inspec Testing; BAE will change BAE, etc.).

NOTE: PEN AND INK CHANGES FOR ENCLOSURE 2 AND ENCLOSURE 3 DO NOT REQUIRE A FORMAL PCP REVISION.

## DIRECT KNOWLEDGE

### A briefing will be conducted prior to beginning work to ensure personnel accomplishing this procedure have direct knowledge of the requirements of this procedure and the safety requirements of the job.  Accomplishment of the briefing will be documented on Appendix 1.

### Method utilized to ensure complete knowledge of the job:

#### All personnel shall have a thorough knowledge of this procedure and complete understanding of the system being worked, prior to starting work.

#### All personnel shall have the ability to foresee and resolve potential problem areas, and to complete the job in a timely yet efficient manner.

# section 3 PROCESS DESCRIPTION

## MATERIAL/EQUIPMENT

### Fabrication Equipment: Welding Machine properly grounded per 009-12 (Welding, Fabrication, and Inspection Requirements; accomplish) of Reference (a), Welding Leads, Torch, Stinger, Portable Rod Oven/Rod Pouch, Pre/Post heat devices.

### Inspection and Repair Equipment as prescribed in approved weld and inspection procedures Acid resistant pump with associated hoses, fittings, and manifold

### Consumables: Weld Rod/filler material, Shielding Gas, Torch Gas

### Temperature Measuring Devices (Preheat and Interpass)

### General Hand Tools as Required

### Approved Cleaning Solvent

## SAFETY EQUIPMENT

### Ventilation (as required by Marine Chemist Certification)

### Respiratory Protection: (When required)

### Safety Clothing (PPE)

### Welding Hood with Flash Burn Protection

### Eye Protection

### Gloves/long sleeve shirt (recommended)

### Proper fire extinguishing agent

### Fire Protection Covering

## SAFETY PRECAUTIONS

### Accomplish the requirements of 009-03, (Toxic and Hazardous Substances; Control) of Reference (a).

### Accomplish the requirements of 009-07, (Confined Space Entry, Certification, Fire Prevention and Housekeeping; accomplish) of Reference (a).

#### A Certified Marine Chemists shall inspect and test the space initially to certify it is safe for workers to enter and safe for hot work. A competent Person must visually inspect and test each certified spaces daily or as often as needed prior to entry and/or hot work by employees on a daily basis.

#### The Marine Chemist Certificate will be posted at designated areas in the affected space.

### Fire Watch must be posted in all affected spaces.

### Accomplish the requirements of 009-24, (Tag out, Isolation, Blanking, and Tagging Requirements; accomplish) of Reference (a).  Work Authorization Form (WAF) shall be obtained and system isolated and tagged out.

### Ensure piping system to be worked is drained and depressurized by ships force prior to cutting out piping.

### Accomplish the requirements of NAVSEA Standard Item 009-06, (Maintaining Protection and Cleanliness from Non-Radioactive Contaminate-Producing Operations; accomplish) of Reference (a).

#### PREVENTION OF LOSS OF CLEANLINESS: Use blanking, plugging or temporary covering, Foreign Matter Exclusion (FME) on open piping and/or components affected by this repair process to maintain system cleanliness IAW NAVSEA Standard Items 009-06, 009-24 of Reference (a).

### Cleanliness Closures shall remain in place except during the time when production work is actually in progress and the opening must actually be uncovered to perform the work.

### When welding Stainless Steel or Chrome-Moly base materials (S-3A thru S-8), Review and accomplish company policy and procedures for Hexavalent Chrome. (Note: Prime Contractor Policy may take precedence over Sub-Contractor Policy during shipboard work).

### When required, accomplish the requirements of 009-112 (Prevention of Radiographic-Inspection Ionizing-Radiation Hazards; accomplish) of Reference (a) for Radiographic Testing (RT), this shall include the submission of Attachment “A” no later than 5 working days prior to the scheduled test date.

## PREPARATION

### Stage all required Materials for verification at the Start of Procedure Checkpoint.

## START OF PROCEDURE

## CHECKPOINT (V)(G) "START OF PROCEDURE"

### Start of this procedure is a CHECKPOINT IAW Paragraph 3.4 of NAVSEA Standard Item 009-09 Process Control Procedure (PCP) Reference (a).  Notify the QA office 4 hours prior to starting this procedure.

### Identification of material shall be visually verified at the point of initial fabrication as being the same material identification or an approved alternate material identification as required by the installation plan,  work item, and Para 5.3.1 of Reference (b).

### When welding Stainless Steel or Chrome-Moly base materials (S-3A thru S-8) notify the Prime Contractor Safety Department and accomplish company policy and procedures for Hexavalent Chrome (Note: Prime Contractor Policy may take precedence over Sub-Contractor Policy during shipboard work).

## FIT-UP REQUIREMENTS

### Components shall be fitted and aligned in accordance with applicable plans and documented on Appendix (4). This alignment shall be maintained throughout the welding process. All Fit-Ups shall be within design tolerances shown on the applicable joint design(s) Appendix (5).

### When a P-3 weld joint design is used and it has been determined that a step down backing ring is required to properly fit-up the weld joint (within the parameters of Reference (h), a revision of this PCP shall be submitted prior to fit-up. Dimensions of the internal pipe diameters and the step backing ring shall be documented on Appendix (10) and included in the revision (Step dimension shall not exceed .250”).

#### Butt welding ends of valves/components shall have a 4:1 pipe taper IAW joint design (P-3).

### Each weld joint shall be physically marked with the weld joint number to ensure traceability of the weld joint numbers from the records to the hardware in accordance with Appendix (6) and Reference (b). The marking shall be made on the thicker member base material (fitting, valve, etc). All weld joint numbers will be documented on Appendix (4) and Appendix (8).

### Pipe bending technique; All pipe bending shall be accomplished in accordance with the requirements of Reference (g). All bend radiuses (from the center of the curvature to the center (axis) of the pipe) shall be in accordance with the work specifications.

#### All pipe bends radius 5D or greater do not require an approved being procedure.

#### All bend radius less than 5D but not less than 2D (D= Pipe Diameter) shall be accomplish by an approve pipe bending procedure in accordance with Reference (g).

### Document pipe bends on Self-Provided Pipe Bend Record Form and include as part of this PCP Enclosure when applicable.

#### Pipe bending acceptance criteria shall be in accordance with paragraph 5.9 of Reference (g).

## CLEANING REQUIREMENTS

### Surfaces to be welded and adjacent surfaces for a distance of approximately one inch (1”) from the weld area shall be clean, dry and free of surface matter or defects such as paint, oil, grease, moisture, scale, oxide, or rust, and objectionable nicks, gouges, and irregularities, to an extent that weld soundness will not be detrimentally affected.

### Use blanking or temporary covering on open piping and components to maintain system cleanliness IAW 009-24 of Reference (a). All new and disturbed surfaces of P-1 piping systems shall be visually free of grease, oil, flux, scale, dirt, loose particles, and any other contamination foreign to the base metal. Tap water residues and light superficial rust on carbon steel surfaces, caused by short time exposure to the atmosphere, are permitted.  Light dust on cleaned surfaces is not objectionable, provided that the quantity and size of the particle does not adversely affect system operations.

## WELDING TECHNIQUE

### P-1 Piping components shall be fabricated in accordance with the workmanship requirements of Reference (b) utilizing Appendix (2). All welds shall be uniquely identified on Appendix (6) and documented on Appendix (8). All defect repairs shall be documented on Appendix (9).

### Excavations in base metal requiring welding will be VT5X/MT or PT Inspected prior to welding IAW Reference (b) Paragraph 7.7.2.

## WELD INSPECTION REQUIREMENTS

### NDT Inspections shall be accomplished IAW Appendix 3. NDT Inspection Acceptance Criteria shall be IAW Reference (e). All weld/NDT inspections shall be documented on Appendix (8). All defect repairs shall be documented on Appendix (9).

### All NDT (G) Checkpoints shall be called out to include SWRMC NDT Examiners at SWRMC.NDTCHECKPOINT@navy.mil.

## (I) CHECKPOINT “VISUAL INSPECTION”

### Checkpoints are required for all NDT visual (VT, VT5X) and RT weld inspections in accordance with NAVSEA Standard Item 009-12 Reference (a). Acceptance Criteria shall be IAW Reference (e).

### (I)(G) CHECKPOINT “NDT INSPECTION”

### NDT inspections (PT, MT, UT, RT) indicated on Appendix (3) shall be in accordance with References (a) and (b) and accomplished in accordance with Reference (d). Acceptance Criteria shall be IAW Reference (e).  Non-applicable NDT will not be deleted but one lined.

#### Accomplish PT IAW Reference (a) Table 1 Column A, line 13.

#### Accomplish MT IAW Reference (a) Table 1 Column A, line 14.

#### Accomplish UT IAW Reference (a) Table 1 Column A, line 12.

#### Accomplish RT IAW Reference (a) Table 1 Column A, line 11.

### (I)(G) CHECKPOINT “NDT INSPECTION” (When Invoked)

### Elevated NDT Option: Accomplish VT/PT of the root layer per Option 1 of Appendix (3) when invoked. Acceptance Criteria shall be IAW Reference (e).

### (I)(G) CHECKPOINT “EVALUATION OF RT FILM”

### Check point for Radiographic Film Interpretation shall be accomplished in accordance with paragraph 3.6 of NAVSEA Standard Item 009-12 of Reference (a). Acceptance Criteria shall be IAW Reference (e).

## PREHEAT AND INTERPASS TEMPERATURE

### The welding surface shall be moisture free

### If required, preheat temperature shall be in accordance with Appendix (2). The maximum interpass temperature shall be listed on Appendix (2).

### Each weld preheat and interpass measurements shall be recorded and documented on Appendix 7 as required by Reference b and Appendix 2 for all weld layers as applicable.

#### Weld layer as defined by Joint Fleet Maintenance Manual consists of Tack, Root, Intermediate, and Final.

#### Record the highest achieved temperature for each layer.

### Surface temperature preheat and interpass temperatures shall be verified by periodic checks using such indicating devices as crayons or electrical potentiometers or other approved devices. Use of low melting metallic alloys for temperature measurement is prohibited. Crayon marks shall be located a minimum of 1 inch away from the weld area.

## PRESSURE TESTING

## (I)(G) CHECKPOINT “HYDROSTATIC TESTING”, OR “OPERATIONAL PRESSURE TESTING” (WHEN OPTION 1 IS INVOKED)

### Hydrostatic testing or Operational Pressure testing (when Option 1 is invoked) shall be in accordance with NAVSEA Standard Item 009-71 of Reference (a) and accomplished as indicated on Appendix (3) and as directed in Enclosure (4) (as applicable). Document results of test on Enclosure (4).

## INSPECTION/DOCUMENTATION FORMS

### PCP Direct Knowledge Attendance Form (Appendix 1)

### Fitup Inspection Record (Appendix 4)

### Weld In-Process Control/Non Destructive Test Record (Appendix 8)

### Weld Defect Repair Record (Appendix 9)

### Checkpoint/Inspection Notification Forms (Contractor Provided)

## OBJECTIVE QUALITY EVIDENCE

### This procedure and all completed documentation (installation and inspection) forms comprise Objective Quality Evidence and traceability of materials and components. This OQE is a formal contract deliverable and shall be delivered to Quality Assurance for review and further disposition, per paragraph 3.5 of 009-09 (Process Control Procedure; Provide and Accomplish) of Reference (a).

## CONTROL OF PROCEDURE

### A copy of the approved procedure shall be at the work site in the possession of the project manager, foreman and/or lead man, during the performance of the work.

# SECTION 4 HAZARDOUS MATERIAL

## HAZARDOUS MATERIALS

### Hazardous material (HAZMAT):

#### Cleaning Solvent (Isopropyl Alcohol, Acetone)

### Hazardous waste

#### Solvent soaked rags

    - Hazardous waste disposal

#### All waste generated will be disposed in accordance with local, state and federal regulations.

#### Every effort will be made to limit the quantity of hazardous waste generated, i.e. the re-use of wiping rags, etc.

PCP DIRECT KNOWLEDGE ATTENDANCE FORM

| Description Of Briefing: |  | Date: | PCP No.: |
| --- | --- | --- | --- |
| Ship/Hull: | Job# |  | Item# |

Instructors: Please retain with completed PCP

| No. | Attendee Name (Print or type) | Dept # | Badge # | Initials | Attendee Signature (Ink only) |
| --- | --- | --- | --- | --- | --- |
| 1. |  |  |  |  |  |
| 2. |  |  |  |  |  |
| 3 |  |  |  |  |  |
| 4. |  |  |  |  |  |
| 5. |  |  |  |  |  |
| 6. |  |  |  |  |  |
| 7. |  |  |  |  |  |
| 8. |  |  |  |  |  |
| 9. |  |  |  |  |  |
| 10. |  |  |  |  |  |
| 11. |  |  |  |  |  |
| 12. |  |  |  |  |  |
| 13. |  |  |  |  |  |
| 14. |  |  |  |  |  |
| 15. |  |  |  |  |  |
| 16 |  |  |  |  |  |
| 17. |  |  |  |  |  |
| 18. |  |  |  |  |  |
| 19. |  |  |  |  |  |
| 20. |  |  |  |  |  |

| Print Instructor Name (Company Name): | Instructor Signature: |
| --- | --- |

APPENDIX 1

A-1-1

WELD TECHNIQUE SHEET

| SHIP: | HULL# | ITEM# | JOB# | PCP# |
| --- | --- | --- | --- | --- |
| SYSTEM/DESCRIPTION |  |  |  |  |

Weld Procedure(s)

| Procedure # |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  |  |  |  |  |  |  |  |  |  |  |
| Base Material Combination |  |  |  |  |  |  |  |  |  |  |  |
| Filler Material(s) |  |  |  |  |  |  |  |  |  |  |  |
| Thickness Range Qualified |  |  |  |  |  |  |  |  |  |  |  |
| Amps |  |  |  |  |  |  |  |  |  |  |  |
| Volts |  |  |  |  |  |  |  |  |  |  |  |
| Polarity |  |  |  |  |  |  |  |  |  |  |  |
| Shielding gas / Flow rate |  |  |  |  |  |  |  |  |  |  |  |
| Purge gas / Flow rate |  |  |  |  |  |  |  |  |  |  |  |
| Preheat / Interpass temp |  |  |  |  |  |  |  |  |  |  |  |
| Preheat Maintenance |  |  |  |  |  |  |  |  |  |  |  |
| Joint #’s welded with this procedure. |  |  |  |  |  |  |  |  |  |  |  |
| Joint design applicable to this procedure |  |  |  |  |  |  |  |  |  |  |  |
| PWHT | Holding temp |  |  | Heating method | Rate of heating |  | Hold time |  |  | Cooling rate |  |
| Proc. # |  |  |  |  |  |  |  |  |  |  |  |
| Base Material name |  |  | Letter# / size / thickness |  |  | Class or type |  | Applicable Document |  |  |  |
| Component A: |  |  |  |  |  |  |  |  |  |  |  |
| Component B: |  |  |  |  |  |  |  |  |  |  |  |
| Component C: |  |  |  |  |  |  |  |  |  |  |  |
| Component D: |  |  |  |  |  |  |  |  |  |  |  |
| Component E: |  |  |  |  |  |  |  |  |  |  |  |
| Component F |  |  |  |  |  |  |  |  |  |  |  |
| Component G |  |  |  |  |  |  |  |  |  |  |  |
| Component H |  |  |  |  |  |  |  |  |  |  |  |
| Component J |  |  |  |  |  |  |  |  |  |  |  |
| Component K |  |  |  |  |  |  |  |  |  |  |  |
| Component L |  |  |  |  |  |  |  |  |  |  |  |
| Component M |  |  |  |  |  |  |  |  |  |  |  |
| Filler Material name |  |  | Group# / size |  |  | type |  | Applicable Document: |  |  |  |
| Filler A: |  |  |  |  |  |  |  |  |  |  |  |
| Filler B: |  |  |  |  |  |  |  |  |  |  |  |
| Filler C: |  |  |  |  |  |  |  |  |  |  |  |

COMMENTS: _____________________________________________________________________________________

APPENDIX 2

A-2-1

WELD INSPECTION AND TESTING REQUIREMENTS

All piping welds shall be one of the following:

REQUIRED:

- Non-Destructively Tested (NDT) and Hydrostatically Tested as required by either Referenced

Ship Installation / Alteration Drawings, NSTP 278 (Requirements for Fabrication Welding

and Inspection, and Casting Inspection and Repair for Machinery, Piping, and Pressure

Vessels) or NSTM Chapter 505.

OPTION 1:

- Request permission from the Supervisor to perform the “enhanced“ NDT requirements via IDR/CFR. VT & PT the root layer per paragraph 3.1.2 of NAVSEA STD Item 009-71 (Testing Requirements for Piping Systems) in lieu of the hydrostatic test. VT & PT the final weld layer per paragraph 3.1.3 of NAVSEA STD Item 009-71. Finally, conduct visual inspection on the affected welds for leakage during the first pressurization to nominal operating pressure as described in paragraph 505-11.1.2.6(b) of S9086-RK-STM-010/CH-505, piping systems as referenced in 009-71. When approved, the IDR/CFR with Government response shall be included as Enclosure 1.

|  | INSPECTION AND Testing Requirement |
| --- | --- |
| NDT Root Pass | VT, PT, VT(5X), MT, RT, |
| NDT Final Pass | VT, PT, MT, RT, ( 60 degrees / 360 degrees ) |
| Hydrostatic Testing | Yes No Hydro pressure______________________ Test Duration_________________________ |
| Operating Pressure Test | Yes Not Applicable |
| IDR # Requesting Option | Approved Not Applicable |

REMARKS:

APPENDIX 3

A-3-1

PIPE FIT-UP INSPECTION RECORD

| SHIP: | HULL: | JOB # |  | PCP# |
| --- | --- | --- | --- | --- |
| ITEM # | MOD # | PARA # | SYSTEM: |  |

| ##### REFERENCE TECHNICAL MANUAL S9074-AR-GIB-010/278 PARA. 4.1.3 REF (b) CHECK INSTRUMENTATION USED FOR INSPECTION |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WIRE /PIN GAUGE BLADE FEELER GAUGE COMBINATION PROTRACTOR BEVEL PROTRACTOR RADIUS GAUGE ##### 6” RULE VERNIER/ DIAL CALIPER Calibration Due Date ________________ S/N________________ MICROMETER Calibration Due Date ___________ S/N___________ |  |  |  |  |  |  |  |  |  |  |  |  |  |
| JOINT ID NO. | MILSTD 22D JOINT DESIGN 2/ | SCRIBE LINE YES OR NO | PROVIDE DIAMETRICAL CLEARANCE MEASUREMENTS .065” MAX 3/ | ALIGN [SAT OR UNSAT] | END GAP 1/16-- 1/8(NEW), 1/32” – 1/16 (REUSED) T+1/16(P-42) /3 | BEVEL LAND 3/ | BEVEL ANGLE 3/ | ROOT OPENING 3/ | PILOT DIAMETER 3/ |  | DATE ACCOMPLISHED | FIT UP INSPECTOR SIGNATURE /BADGE NO. 1/ |  |
| Comments: _______________________________________________________________________________________________ ________________________________________________________________________________________________ |  |  |  |  |  |  |  |  |  | Note: Use comment section for any Fitting not covered. |  |  |  |

NOTE:  All blanks must be filled in.  If not applicable, write N/A.

1/   The person signing for this block is also signing in acknowledgement that the material has been identified per paragraph 3.5.2 of this PCP.

2/   Document the reuse of fittings and pipe on Appendix (4) continuation page

3/   All measurements shall be in accordance with MIL-STD- 22D Reference (c)

APPENDIX 4

A-4-1

PIPE FIT-UP INSPECTION RECORD (P-73)

| SHIP: |  |  |  | HULL: |  |  | ITEM # |  |  |  | JOB # |  |  | PCP# |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ##### REFERENCE TECHNICAL MANUAL S9074-AR-GIB-010/278 PARA. 4.1.3 REF (b) CHECK INSTRUMENTATION USED FOR INSPECTION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WIRE /PIN GAUGE BLADE FEELER GAUGE COMBINATION PROTRACTOR BEVEL PROTRACTOR RADIUS GAUGE ##### 6” RULE VERNIER/ DIAL CALIPER Calibration Due Date ________________ S/N________________ MICROMETER Calibration Due Date ___________ S/N___________ |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| JOINT ID NO. | MILSTD 22D JOINT DESIGN | PROVIDE DIAMETRICAL CLEARANCE MEASUREMENTSSIDE A, (D DIMN) .031 MAX | PROVIDE DIAMETRICAL CLEARANCE MEASUREMENTS SIDE B, (D DIMN) .031 MAX |  | ALIGN [SAT OR UNSAT] | BEVEL LAND SIDE A, (B DIMN) 1” & BELOW .010” ±.005” |  | BEVEL LAND SIDE B (B DIMN) ABOVE 1” .030”±.005” | BEVEL ANGLE SIDE A (O DIMN) 40° ± 5° | BEVEL ANGLE SIDE B (O DIMN) 40° ± 5° |  | LATERAL CLEARANCE SIDE A (C DIMN) .031” MAX | DATE ACCOMPLISHED |  |  | FIT UP INSPECTOR SIGNATURE /BADGE NO. 1/ |  |  |
| Comments: _______________________________________________________________________________________________ ________________________________________________________________________________________________ |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Note: Use comment section for any Fitting not covered. |  |  |  |

NOTE:  All blanks must be filled in.  If not applicable, write N/A.

1/   The person signing for this block is also signing in acknowledgement that the material has been identified per paragraph 3.5.2 of this PCP.

2/   Document the reuse of fittings and pipe on Appendix (4) continuation page

3/   All measurements shall be in accordance with MIL-STD- 22D Reference (c)

APPENDIX 4

A-4-2

PIPE FIT-UP INSPECTION RECORD

Re-Use of Fittings and/or Pipe

All re-used fittings and Pipe will be inspected to meet the requirements of Ref b and c. 1/

| Joint No. | Depth of Socket (see Table 1 below) | Diametrical Clearance 1/ | Wall Thickness (TM) | 1/16 max End Gap 2/ | Joint No. | Depth of Socket (see Table 1 below) | Diametrical Clearance 1/ | Wall Thickness (TM) | 1/16 max End Gap 2/ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| N/A |  |  |  |  |  |  |  |  |  |

1/ Reuse of fittings not allowed if the diametrical clearance exceeds 0.065 inch.

2/ NSTM 074 paragraph 074-4.10.1; For Re-use Fittings, The pipe end gap clearance shall be 1/32 to 1/16 inch maximum.

TABLE 1 ANSI/ASME B16.11 MINIMUM SOCKET DEPTH and WALL THICKNESS FOR RE-USED FITTINGS

(NUMBERS IN PARENTHESIS ARE DECIMAL EQUIVALENT IN INCHES)

| 1.FITTING SIZE (INCHES) | 2.MIN DEPTH OF SOCKET (L) | 3.MIN SOCKET DEPTH (L) for 50% SOCKET DEPTH REDUCTION DIAMETRICAL CLEARANCE 0.0 TO 0.025” MAX | MIN SOCKET DEPTH (L) for 25% SOCKET DEPTH REDUCTION DIAMETRICAL CLEARANCE .026 THRU .065 MAX | MIN SOCKET WALL THICKNESS (W) CLASS 3000# | MIN SOCKET WALL THICKNESS (W) CLASS 6000# |
| --- | --- | --- | --- | --- | --- |
| 1/8 | 3/8 (.375”) | 3/16 (.1875”) | 9/32 (.2812”) | 1/8 (.125”) | 1/8 (.125”) |
| 1/4 | 3/8 (.375”) | 3/16 (.1875”) | 9/32 (.2812”) | 1/8 (.125”) | 3/16 (.1875”) |
| 3/8 | 3/8 (.375”) | 3/16 (.1875”) | 9/32 (.2812”) | 1/8 (.125”) | 3/16 (.1875”) |
| 1/2 | 3/8 (.375”) | 3/16 (.1875”) | 9/32 (.2812”) | 3/16 (.1875”) | 3/16 (.1875”) |
| 3/4 | 1/2 (.500”) | 1/4 (.250”) | 3/8 (.375”) | 3/16 (.1875”) | 1/4 (.250”) |
| 1 | 1/2 (.500”) | 1/4 (.250”) | 3/8 (.375”) | 3/16 (.1875”) | 1/4 (.250”) |
| 1-1/4 | 1/2 (.500”) | 1/4 (.250”) | 3/8 (.375”) | 3/16 (.1875”) | 1/4 (.250”) |
| 1-1/2 | 1/2 (.500”) | 1/4 (.250”) | 3/8 (.375”) | 3/16 (.1875”) | 5/16 (.3125”) |
| 2 | 5/8 (.625”) | 5/16 (.3125”) | 15/32 (.4687”) | 1/4 (.250”) | 3/8 (.375”) |

APPENDIX 4 (Continued)

A-4-3

THIS SHEET IS ONLY A PLACE HOLDER.

PLEASE REPLACE IT WITH OF

JOINT DESIGN PAGE(S) FROM MIL-STD-22D

APPENDIX 5

A-5-1

| ###### JOINT MAP |  |  |  |  |  | Page __of ___ |
| --- | --- | --- | --- | --- | --- | --- |
| ###### (Insert Joint Mapping Plan) |  |  |  |  |  |  |
| 1. SHIP | 2. HULL NO. | 3. ITEM NO. |  | 4. PCP NO. | 5. JOB NO. |  |
| 6. DESCRIPTION: |  |  |  |  |  |  |
| 7. JOINT DESIGN: | 8. PIPE SIZE(S): |  | 9. REQUIRED FILLET SIZE(S): |  |  |  |

APPENDIX 6

A-6-1

Preheat/Interpass Temperature Record

| SHIP: USS | HULL# |  | ITEM# | JOB# | PCP# |
| --- | --- | --- | --- | --- | --- |
| Calibrated Equipment: |  | ID#: |  | Cal Due Date: |  |
| 1. Enter the layer of welding (i.e., tacks, root, intermediate, and final). |  | 2. Enter the actual preheat temperature as measured just prior to welding |  | 3. Enter the maximum interpass temperature as measured during the process. |  |

| Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) | Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Tack |  |  |  |  |  | Tack |  |  |  |
|  |  | Root |  |  |  |  |  | Root |  |  |  |
|  |  | Intermediate |  |  |  |  |  | Intermediate |  |  |  |
|  |  | Final |  |  |  |  |  | Final |  |  |  |
| Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) | Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) |
|  |  | Tack |  |  |  |  |  | Tack |  |  |  |
|  |  | Root |  |  |  |  |  | Root |  |  |  |
|  |  | Intermediate |  |  |  |  |  | Intermediate |  |  |  |
|  |  | Final |  |  |  |  |  | Final |  |  |  |
| Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) | Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) |
|  |  | Tack |  |  |  |  |  | Tack |  |  |  |
|  |  | Root |  |  |  |  |  | Root |  |  |  |
|  |  | Intermediate |  |  |  |  |  | Intermediate |  |  |  |
|  |  | Final |  |  |  |  |  | Final |  |  |  |
| Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) | Joint # | Date | Weld layer(1) | Preheat (2) | Interpass (3) | Welder Signature(4) |
|  |  | Tack |  |  |  |  |  | Tack |  |  |  |
|  |  | Root |  |  |  |  |  | Root |  |  |  |
|  |  | Intermediate |  |  |  |  |  | Intermediate |  |  |  |
|  |  | Final |  |  |  |  |  | Final |  |  |  |

NOTE: 1. Weld layers may be deleted when not required. 
NOTE: 2. Two layer welds will have root and final only and fillets welds may have only tack and finals).

Appendix 7

A-7-1

WELD IN-PROCESS CONTROL/NON-DESTRUCTIVE TEST RECORD    (TO DOCUMENT WELDING IN-PROCESS AND NDT INSPECTION RESULT)

| 1. SHIP: USS |  |  |  |  |  |  |  | 2. HULL# |  |  | 3. ITEM# |  |  |  |  |  |  |  |  | 4.JOB# |  |  |  |  |  |  | 5. PCP# |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9. BRIEF DESCRIPTION (TITLE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 10. NDT ACCEPTANCE CLASS: |  |  |  | 1 2 3 (MIL-STD-2035A) |  |  |  |  |  |  |  |  | Acceptance IAW MIL-STD-2035A(SH) Reference (e) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| JOINT INFORMATION |  |  |  |  |  |  |  | ROOT PASS |  |  |  |  |  |  |  |  |  |  |  |  | FINAL PASS |  |  |  |  |  |  |  |
| JOINT ID | COMPONENT A |  | SIZE |  | JOINT DESIG |  |  |  | WELDER NAME 4/ |  |  | ROOT INSP |  |  | ACC REJ 1/ |  |  | NDT INSPECTOR |  |  | WELDER NAME 4/ |  | FINAL INSP |  |  | ACC/ REJ 1/ 3/ |  | NDT INSPECTOR 2/ |
|  | COMPONENT B |  |  |  |  |  |  |  | DATE WELDED |  |  |  |  |  |  |  |  | INSPECT DATE |  |  | DATE WELDED |  |  |  |  |  |  | INSPECT DATE |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
| PT TECHNIQUE |  |  |  |  |  | VT INSPECTION |  |  |  |  |  |  |  |  |  | MT METHOD |  |  |  |  |  | MT (CONT’D) |  |  |  |  |  |  |
| PENETRANT TYPE II |  |  |  |  |  | VT5X |  |  |  |  |  |  |  |  |  | DRY CONTINUOUS |  |  |  |  |  | MT PARTICLES COLOR: RED OTHER ________ |  |  |  |  |  |  |
| MANUFACTURER MAGNAFLUX OTHER______ |  |  |  |  |  | DIMENSIONAL |  |  |  |  |  |  |  |  |  | CIRCULAR LONGITUDINAL |  |  |  |  |  | MANUFACTURER MAGNAFLUX OTHER_______ |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | YOKE PROD OTHER |  |  |  |  |  | MT INSTRUMENT MODEL: |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CURRENT: AC HWDC |  |  |  |  |  |  |  |  |  |  |  |  |
| PT INSPECTION PROCEDURE: |  |  |  |  |  | VT INSPECTION PROCEDURE: |  |  |  |  |  |  |  |  |  | MT INSPECTION PROCEDURE: |  |  |  |  |  | RT INSPECTION PROCEDURE |  |  |  |  |  |  |
| UT TECHNIQUE |  |  |  |  |  |  | UT (CONT’D) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| UT THICKNESS STRAIGHT BEAM |  |  |  |  |  |  | UT SHEARWAVE |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| UT INSPECTION PROCEDURE: |  |  |  |  |  |  | UT INSPECTION PROCEDURE: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | PRINTED NAME |  |  |  |  |  |  |  | SIGNATURE4/ |  |  |  |  |  |  |  |  | PRINTED NAME |  |  |  |  |  | SIGNATURE |  |  |  |
| WELDER NO. 1 |  |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 2 |  |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 3 |  |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 4 |  |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

NOTES:  1. REJECTED WELD JOINTS SHALL BE REPAIRED AND DOCUMENTED ON WELD DEFECT REPAIR FORM (APPENDIX 8).

2. THE INSPECTOR ACCEPTING WELDS CERTIFIES BY PERSONAL OBSERVATION THAT THE WELD FILLET SIZE IS SATISFACTORY AS APPLICABLE.

3. SEE RADIOGRAPHIC TEST (RT) AND/OR ULTRASONIC TEST (UT) REPORT FOR INSPECTION RESULTS AS APPLICABLE.

4. Welder’s initial and signature indicate all weld parameters of appendix 2 have been verified.

5. 5XMAGNIFICATION VISUAL INSPECTIONS OF ROOT WELD LAERS MAY BE PERFORMED BY QUALIFIED PRODUCTION PERSONNEL. (TM278 PARA. 4.1.3.1 applies).

APPENDIX 8

A-8-1

WELD IN-PROCESS CONTROL/NON-DESTRUCTIVE TEST RECORD (cont)  (TO DOCUMENT WELDING IN-PROCESS AND NDT INSPECTION RESULT)

| 10. NDT ACCEPTANCE CLASS: |  |  |  |  | 1 2 3 Class 1 Acceptance IAW MIL-STD-2035A(SH) Reference (e) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| JOINT INFORMATION |  |  |  |  | ROOT PASS |  |  |  |  |  |  |  |  |  | FINAL PASS |  |  |  |  |  |  |  |
| JOINT ID | COMPONENT A |  | SIZE | JOINT DESIG |  | WELDER NAME4/ | ROOT INSP |  |  | ACC REJ 1/ |  | NDT INSPECTOR |  |  | WELDER NAME4/ |  | FINAL INSP |  |  | ACC/ REJ 1/ 3/ | NDT INSPECTOR 2/ |  |
|  | COMPONENT B |  |  |  |  | DATE WELDED |  |  |  |  |  | INSPECT DATE |  |  | DATE WELDED |  |  |  |  |  | INSPECT DATE |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
|  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |
| PT TECHNIQUE |  |  |  |  |  | VT INSPECTION |  |  |  |  | MT METHOD |  |  |  |  |  | MT (CONT’D) |  |  |  |  |  |
| PENETRANT TYPE II |  |  |  |  |  | VT5X |  |  |  |  | DRY CONTINUOUS |  |  |  |  | MT PARTICLES COLOR: RED OTHER________ |  |  |  |  |  |  |
| MANUFACTURER MAGNAFLUX OTHER______ |  |  |  |  |  | DIMENSIONAL |  |  |  |  | CIRCULAR LONGITUDINAL |  |  |  |  | MANUFACTURER MAGNAFLUX OTHER_______ |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | YOKE PROD OTHER |  |  |  |  | MT INSTRUMENT MODEL: |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | CURRENT: AC HWDC |  |  |  |  |  |  |  |  |  |  |  |
| PT INSPECTION PROCEDURE: |  |  |  |  |  | VT INSPECTION PROCEDURE: |  |  |  |  | MT INSPECTION PROCEDURE: |  |  |  |  | RT INSPECTION PROCEDURE |  |  |  |  |  |  |
| UT TECHNIQUE |  |  |  |  |  | UT (CONT’D) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| UT THICKNESS STRAIGHT BEAM |  |  |  |  | UT SHEARWAVE |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| UT INSPECTION PROCEDURE: |  |  |  |  | UT INSPECTION PROCEDURE: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | PRINTED NAME |  |  | SIGNATURE |  |  |  |  |  |  |  | PRINTED NAME |  |  |  |  |  | SIGNATURE |  |  |  |
| WELDER NO. 1 |  |  |  |  |  |  |  | NDT INSPECTOR NO. 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 2 |  |  |  |  |  |  |  | NDT INSPECTOR NO. 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 3 |  |  |  |  |  |  |  | NDT INSPECTOR NO. 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 4 |  |  |  |  |  |  |  | NDT INSPECTOR NO. 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

NOTES: 1. REJECTED WELD JOINTS SHALL BE REPAIRED AND DOCUMENTED ON WELD DEFECT REPAIR FORM (APPENDIX 8).

2. THE INSPECTOR ACCEPTING WELDS CERTIFIES BY PERSONAL OBSERVATION THAT THE WELD FILLET SIZE IS SATISFACTORY AS APPLICABLE.

3. SEE RADIOGRAPHIC TEST (RT) AND/OR ULTRASONIC TEST (UT) REPORT FOR INSPECTION RESULTS AS APPLICABLE.

4. Welder’s initial and signature indicate all weld parameters of appendix 2 have been verified.

5. 5XMAGNIFICATION VISUAL INSPECTIONS OF ROOT WELD LAERS MAY BE PERFORMED BY QUALIFIED PRODUCTION PERSONNEL. (TM278 PARA. 4.1.3.1 applies).

APPENDIX 8 Continue

A-8-2

(TO DOCUMENT WELDING IN-PROCESS AND NDT INSPECTION RESULT WITH RT INSPECTIONS)

| 1. SHIP: USS |  |  |  |  |  |  | 2. HULL# |  |  |  |  |  |  |  | 3. ITEM# |  |  |  |  | 4. JOB# |  |  | 5. PCP# |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6. BRIEF DESCRIPTION (TITLE): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7. NDT ACCEPTANCE CLASS: |  |  |  | 1 2 3 (MIL-STD-2035A) |  |  |  |  |  |  |  | Acceptance IAW MIL-STD-2035A(SH) Reference (e) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| JOINT INFORMATION |  |  |  |  |  |  |  | ROOT PASS |  |  |  |  |  |  |  |  |  |  | FINAL PASS |  |  |  |  |  |  |  |
| JOINT ID | COMPONENT A |  | SIZE |  | JOINT DESIG |  |  |  | WELDER NAME 4/ |  | ROOT INSP |  |  | ACC REJ 1/ |  |  | NDT INSPECTOR |  | WELDER NAME 4/ |  |  | FINAL INSP |  |  | ACC/ REJ 1/ 3/ | NDT INSPECTOR 2/ |
|  | COMPONENT B |  |  |  |  |  |  |  | DATE WELDED |  |  |  |  |  |  |  | INSPECT DATE |  | DATE WELDED |  |  |  |  |  |  | INSPECT DATE |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |
|  | RT Final Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RT |  |  | ACCREJ |  |
|  | Acceptance Only |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |
|  | RT Final Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RT |  |  | ACCREJ |  |
|  | Acceptance Only |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |
|  | RT Final Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RT |  |  | ACCREJ |  |
|  | Acceptance Only |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |
|  | RT Final Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RT |  |  | ACCREJ |  |
|  | Acceptance Only |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |  |  |  |  |  |  |  |  |  | ACCREJ |  |
|  | RT Final Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RT |  |  | ACCREJ |  |
|  | Acceptance Only |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PT TECHNIQUE |  |  |  |  |  | VT INSPECTION |  |  |  |  |  |  |  |  |  | MT METHOD |  |  |  |  | MT (CONT’D) |  |  |  |  |  |
| PENETRANT TYPE II |  |  |  |  |  | VT5X |  |  |  |  |  |  |  |  |  | DRY CONTINUOUS |  |  |  |  | MT PARTICLES COLOR: RED OTHER _________ |  |  |  |  |  |
| MANUFACTURER MAGNAFLUX OTHER_____ |  |  |  |  |  | DIMENSIONAL |  |  |  |  |  |  |  |  |  | CIRCULAR LONGITUDINAL |  |  |  |  | MANUFACTURER MAGNAFLUX OTHER________ |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | YOKE PROD OTHER |  |  |  |  | MT INSTRUMENT MODEL: |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CURRENT: AC HWDC |  |  |  |  |  |  |  |  |  |  |
| PT INSPECTION PROCEDURE |  |  |  |  |  | VT INSPECTION PROCEDURE |  |  |  |  |  |  |  |  |  | MT INSPECTION PROCEDURE |  |  |  |  | RT INSPECTION PROCEDURE |  |  |  |  |  |
|  |  | PRINTED NAME |  |  |  |  |  |  |  | SIGNATURE4/ |  |  |  |  |  |  |  | PRINTED NAME |  |  |  |  |  | SIGNATURE |  |  |
| WELDER NO. 1 |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 2 |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 3 |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| WELDER NO. 4 |  |  |  |  |  |  |  |  |  |  |  |  | NDT INSPECTOR NO. 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |

APPENDIX 8 Continue

A-8-3

| ### WELD DEFECT REPAIR RECORD (TO DOCUMENT WELD JOINT REPAIR AS APPLICABLE) 1. SHIP:; 3. ITEM#; 5.PCP#. 2. HULL:; 4. MOD#; 6. JOINT #:. |
| --- |
| 9. DEFECT DESCRIPTION (CHECK ALL THAT APPLY) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CRACK |  | INCOMP INSERT FUSION |  |  |  |  | INCOMPLETE FUSION |  |  |  | ARC STRIKE |  |  |  |  | ROUNDED |
| SLAG |  | CRATER PIT |  |  |  |  | BURN THRU |  |  |  | WELD SPLATTER |  |  |  |  | SHORT LEG SIZE |
| POROSITY |  | INTERNAL CONCAVITY |  |  |  |  | MELT THRU |  |  |  | ROOT EDGE FUSION COND |  |  |  |  | OTHER: (ENTER BELOW) |
| UNDERCUT |  | INTERNAL CONVEXITY |  |  |  |  | TUNGSTEN |  |  |  | LINEAR |  |  |  |  |  |
| OXIDATION |  | CENTERLINE CREASE |  |  |  |  | INCOMPLETE PENETRATION |  |  |  | LINEAR DISPOSED |  |  |  |  |  |
| 10. DEFECT LOCATION(S) AND EXTENT SEE SKETCH IN REMARKS |  |  |  |  |  |  |  |  |  |  | 11. INSPECTOR (SIGNATURE/DATE) |  |  |  |  |  |
| ### 12. DEFECT REPAIR. REPAIR CYCLES 1 2 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 13. TYPE OF REPAIR GRIND ONLY GRIND AND WELD WELD ONLY OTHER (SEE REMARKS) |  |  |  | 14. REPAIR LOCATION(S) AND EXTENT SEE SKETCH IN REMARKS |  |  |  | 15. WELD PROC AND REV/CH NA SAME AS ORIGINAL (APP 2) |  |  |  | 16. EXCAV NDT REQUIRED YES (MARK REQD INSP BLK 24/25) NO |  |  | 17. ROOT PASS INSP REQUIRED YES (MARK REQD INSP BLK 24/25) NO |  |
| 18. LAYER T/R/I/F | 19. FILLER TYPE |  |  |  | 20. FILLER SERIAL NO. (MIC NO.) |  |  |  | 21. PREHEAT/ INTERPASS TEMP |  |  | 22 WELDER (SIGNATURE/PRINT/DATE) |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SAT |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SAT |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | SAT |  |  |  |  |  |  |  |
| - 23. REPAIR NDT INSPECTIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| REPAIR WELD REQUIRES THE SAME INSPECTIONS AS THE ORIGINAL WELD. CARRY OVER REJECTED OR VOIDED INSPECTIONS FROM WELDING IN-PROCESS CONTROL/ NDT RECORD (APPENDIX 7). EXCAVATION (R) ROOT (I) INTERMEDIATE (F) FINAL (T) TACKS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 24. INSPECTION |  |  | 25 INSPECTION TYPE |  |  |  |  |  | 26. PROCEDURE USED |  |  |  | 27. INSPECTOR (SIGNATURE/PRINT/DATE) |  |  |  |
| EXCAV NA |  |  | 5X PT TYPE IIC MT/EQUIP NO.: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| ROOT NA |  |  | VT 5X PT TYPE IIC MT/EQUIP NO.: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| BACKGOUGE NA |  |  | 5X PT TYPE IIC MT/EQUIP NO.: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| PT/MT ( I ) NA |  |  | PT TYPE IIC MT/EQUIP NO.: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| VT (F) NA |  |  | OUTSIDE (ALL VTs) INSIDE ACCESSIBLE INSIDE PARTIAL INSIDE INSP |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| PT/MT(F) NA |  |  | PT TYPE IIC 24 HOUR MT/EQUIP NO.: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| PT/MT – ID(F) NA |  |  | PT TYPE IIC MT/EQUIP NO.: INACCESSIBLE PARTIAL INSP DONE |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| UT NA |  |  | SERIAL # RANGE CALIBRATION DATE: |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| RT (F) NA |  |  | 60O 360O 100% |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| FILLET SIZE (F) N/A |  |  |  |  |  |  |  |  |  |  |  |  | SAT REJ |  |  |  |
| NDT PROCEDURE : VT: |  |  |  |  |  | NDT PROCEDURE : PT: |  |  |  | NDT PROCEDURE: MT: |  |  |  | NDT PROCEDURE: RT: |  |  |
| 28. REMARKS (SKETCHES) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

APPENDIX 9

A-9-1

WELDED JOINT BACKING RING DIMENSIONS

TO DOCUMENT STEP TYPE BACKING RING DIMENSIONS (WHEN APPLICABLE)

| 1. SHIP: | 3. ITEM# | 5. PCP# |
| --- | --- | --- |
| 2. HULL: | 4. MOD# | 6. JOINT# |

TABLE 1

| RING TYPE | DIM | 2” IPS OR LESS | OVER 2” IPS |
| --- | --- | --- | --- |
|  | T | 1/8” +1/32” MINUS 0” | 3/16” MAX |
| FLAT | W | 3/4” ±1/32” | 1” +1/32” MINUS 0” |
|  | L | 1/16” APPROX | 1/16” +1/32” MINUS 0” |
|  | B | 3/32” APPROX 45° CHAMFER | 3/16” ± 1/32 |

| PIPE AND COMPONENT (ID) INSIDE DIAMETERS: |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 1. INSIDE DIAMETER I.D “A”: ____________________________________ ( ) PIPE ( ) FITTING /VALVE |  | 2. INSIDE DIAMETER I.D. “C”: _______________________________ ( ) PIPE ( ) FITTING /VALVE |  | 3. DIFFERENCE OF 1 & 2 (Not to exceed 1/4" (0.250”)): ___________________________________ |  |
| NEW (MANUFACTURED) STEP BACKING RING DIMENSIONS: (DIMENSIONS T, W, L, AND B ON TABLE 1 ABOVE MUST BE ADHERED TO) |  |  |  |  |  |
| 4. RING OUTSIDE DIAMETER “A” |  |  | 5. RING OUTSIDE DIAMETER “C” |  | 6. DIFFERENCE OF “4” & “5” |
| 7. WALL THICKNESS DIMENSION“T” (see Note 3 below) OD “A”____________ OD “C”____________ |  |  | 8. RING LENGTH DIMENSION “W” ______________________________ |  | 9. CHAMFER STEP DIMENSION “L” __________________________________ |
| 10. CHAMFER LENGTH DIMENSION “B” |  |  | 11. STEP RING SERIAL NO. (Marked on the ring, see Note 4 below) |  |  |
| 12. STEP BACKING RING MANUFACTURED BY: (MACHINIST) Print Name _________________________________ Signature _______________________________ Date _________________ |  |  |  |  |  |
| 13. STEP BACKING RING DIMENSIONS VERIFIED BY: (QAI, QCI, NDT INSPECTOR) Print Name _________________________________ Signature _______________________________ Date __________________ |  |  |  |  |  |
| 14. MICROMETER/CALIPER USED | SERIAL#____________________________ CAL DUE: ____________________________ |  |  |  |  |

NOTES

- THE DIFFERENCE OF THE INSIDE DIAMETERS OF PIPE AND COMPONENT MUST NOT EXCEED 	0.250” 	(1/4” INCH) IAW GSO SECTION 074.d.

- THE INSIDE DIAMETER OF THE RING MUST BE STRAIGHT. THE WALL THICKNESS DIMENSION (“T”) 	FOR THE SMALLER END SHALL CONFORM TO MIL-STD-22 (FIGURE 63) DIMENSION WHILE THE 	LARGER END WILL HAVE A THICKER DIMENSION TO ACHIEVE A STRAIGHT INSIDE DIAMETER AS 	DIRECTED BY SWRMC CODE 135.

- THE OUTSIDE TRANSITION AREA OF THE RING SHALL BE TAPERED TO A 45 DEGREE ANGLE.

- ALL DIMENSIONS SHALL BE VERIFIED BY A QCI, QAI OR NDT INSPECTOR PRIOR TO 	INSTALLATION.

- THIS RECORD BECOMES PART OF OBJECTIVE QUALITY EVIDENCE (OQE) FOR PCP.

APPENDIX 10

A-10-1